## Slide 1: Scintillator Non-Proportionality: Why a Constant Isn’t a Constant…
William W. Moses
Lawrence Berkeley National Laboratory
October 21, 2011
This work supported by the National Nuclear Security Administration, Office of Defense Nuclear Nonproliferation, Office of Nonproliferation Research and Development (NA-22) of the U.S. Department of Energy under Contract No. DE-AC02-05CH11231.

## Slide 2: Light Yield
Fundamental Scintillator Constant
BGO 8,200 photons/MeV
NaI:Tl 38,000 photons/MeV
CsI:Tl 60,000 photons/MeV
LSO 28,000 photons/MeV
LaCl3:Ce 50,000 photons/MeV
LaBr3:Ce 63,000 photons/MeV

## Slide 3: Non-Proportionality
Light Yield Not Constant
Depends on Particle Energy & Type

## Slide 4: 1950’s: Non-Proportionality First Studied
Alkali Halides (NaI & CsI)
Different Particle Types (, , p, , Light & Heavy Nuclei, Fission Fragments, …)
~4 Orders of Magnitude Energy Range
Question Studied: Why Does Light Yield Depend on Particle Type & Energy?

## Slide 5: Light Yield Correlated with Ionization Density • Mechanism: Saturation of Luminescent Centers
Work Stopped in Late 1960’s
Figure from R. B. Murray & A. Meyer, Phys. Rev. 122, pp. 815–826, 1961
Scintillation Efficiency
(dL/dE)
Ionization Density (dE/dx)

## Slide 6: 1991: LSO Discovered
~4x More Light Than BGO, But Same Energy Resolution
Why Isn’t Resolution Dominated by Counting Statistics?
BGO
LSO
662 keV
9.9% fwhm
662 keV
9.4% fwhm

## Slide 7: 1995: Non-Proportionality Resurrected to Explain Poor Energy Resolution
Interest Growing Steadily (for  spectroscopy / excitation…)

## Slide 8: How Does Non-Proportionality Affect Energy Resolution?
The Onion Model…

## Slide 9: Layer 1: Photon Response

## Slide 10: Initial Interaction: Compton vs. Photoelectric
Non-Proportionality + Multiple Energy Deposit
 Degraded Energy Resolution
Scintillator
Incident Gamma
Photoelectric
Photoelectric
Compton

## Slide 11: Energy Resolution for Small LSO Crystal
• Large Difference in Photoelectric Fraction
• No Difference in Energy Resolution
 There Must Be Something More…
LSO – 1 cm Cube
LSO – 2 mm Cube
662 keV
9.4% fwhm
662 keV
10.7% fwhm

## Slide 12: Photoelectric Interactions
• Usually Occur with Inner Shell Electrons
 Inner Shell Hole Filled via Cascade
K
L
M
Valence
W

photoelectron

## Slide 13: Simplified Cascade Diagram for NaI
Many Energetic (>1 keV) Particles Created
Fluorescent X-Rays & Auger Electrons
83% K-Shell
Interactions
~30 keV
Fluorescent
X-Rays
Different
Photoelectron
Energies
1–4 keV
Auger Electrons
Figure from B.D. Rooney & J.D. Valentine, IEEE Trans. Nucl. Sci. 44, pp. 509–516, 1997

## Slide 14: Cascade After Photoelectric Interaction
Non-Proportionality + Multiple Energy Deposit
 Degraded Energy Resolution
Initial Gamma
Fluorescent X-Ray
Auger Electrons
Photoelectron

## Slide 15: Photon Response
Structure in Photon Response Curve
Includes Many Confounding Effects
Scintillator
Photodetector
10
102
103
1.00
1.13
1.25
1.38
1.50
Energy (keV)
Relative Light Yield
Figure from M. Moszyński, et al., Nucl. Instr. Meth. A-484, pp. 259–269, 2002
Monochromatic Gamma

## Slide 16: Layer 2: Electron Response

## Slide 17: Electron Response
Scintillator
Monochromatic Electron
Photodetector
Surface Effects
Sample Charging

## Slide 18: How Is Electron Response Measured?
662 keV Gamma Compton Scatters in Scintillator
Energy of Scattered Gamma Measured in HPGe
Plot Light Output vs. Electron Energy (E–EHPGe)
Figure from J.D. Valentine, et al., Nucl. Instr. Meth. A-486, pp. 452, 2002
Compton Coincidence Technique

## Slide 19: Compton Interactions
• Usually Occur with Outer Shell Electrons
 All Energy Transferred to e– (No Cascade)
K
L
M
Valence
W

Compton electron

## Slide 20: Electron Response vs. Photon Response
Electron Response Has Less Structure
Photon Response Can Be Qualitatively Predicted from Electron Response & Cascade
Photon Response
10
102
103
1.00
1.13
1.25
1.38
1.50
Photon Energy (keV)
Relative Light Yield
Electron Response
Figure on left from M. Moszyński, et al., Nucl. Instr. Meth. A-484, pp. 259–269, 2002
Data on right from G. Hull, et al., IEEE Trans. Nucl. Sci. 56, pp. 331–336, 2009
0.9
1.0
1.1
1.2
1.3
Relative Light Yield
1
102
103
Electron Energy (keV)
10

## Slide 21: How Is Electron Response Measured?
Synchrotron X-Ray Ejects K-Shell Electron
Measure Light, Subtract “Offset” from K-Shell Filling
Measures Electron Response From Tenths of keV to Tens of keV
Figure from I.V. Khodyuk, et al., J. Appl. Phys. 107, pp. 113513, 2010

E= EK
Photo-electron
(E= 0 keV)
K L M Valence
Total Light =
Light (K-shell hole) +
Light (0 keV electron)

E= EK+1
Photo-electron
(E= 1 keV)
K L M Valence
Total Light =
Light (K-shell hole) +
Light (1 keV electron)
W
NaI:Tl
K-Dip Spectroscopy
W

## Slide 22: Do Primary Compton & Core Holes / Cascade Completely Explain Resolution Degradation?
No!!! There Must Be Something More…
Gamma
Excited
Counting Stats
Electron
Excited
Figure from W.W. Moses, et al., IEEE Trans. Nucl. Sci. NS-55, pp. 1049, 2008
NaI:Tl

## Slide 23: Electron Energy Deposit Still Non-Uniform!
Landau Fluctuations
Delta Ray
e+e– in Bubble Chamber

## Slide 24: Layer 3: Ionization Density

## Slide 25: Yield Depends on Electron Ionization Density
Non-Proportionality + Non-Uniform Energy Deposit
 Degraded Energy Resolution

## Slide 26: Model Fluctuations in Light Output Along the Electron Track
Compute Variance in Light Produced at Each Point
Integrate Variance Along Track To Get Total Variance
Bethe-Block Equation
 Gives ionization density (dE/dx) as function of E
Landau Equation
 Gives variation in ionization density (dE/dx)
Measured Electron Response
 Gives scintillation efficiency as function of E

## Slide 27: Success!!!
Given the Electron Response for a Material, Can Quantitatively Predict the Energy Resolution
Figure from G. Bizarri, et al., Presentation I8-2 at SCINT09, Jeju Island, Korea

## Slide 28: Can We Understand the Shape of the Electron Response Curve?

## Slide 29: What Creates the Shape of the Electron Response Curve?
Key Empirical Observation:
Light Output Depends on Ionization Density
Alkali Halides
Oxides
Decrease at High Ionization Density
(All Materials)
Decrease at Low Ionization Density
(~Only Alkali Halides)

## Slide 30: Competing Processes for e/h Recombination
Many Ways for e/h Pairs in a Voxel to Recombine
Not All Recombinations Produce Light
Processes Depend on Ionization Density
Electron Ionization Track
One Voxel
  Non-Radiative Trapping
  Exciton Formation
  Electron / Hole / Exciton Interactions
  Luminescence
h
e
e
h
e
h
e
h
e
h
e
h
e
h
e
h
h
e
h
e
h
e
h
e
h
e
h
e
e
h
h
e
h
e
h
e
h
h
e
h
e
h
h
e
e
h
h
e

## Slide 31: Pause for Definitions
Exciton: A bound state of a hole and an excited electron
  Moves as a single particle through the lattice
  Frequently de-excites radiatively (by emitting a photon)
Auger Process: Two particles in excited states turn into one particle in an excited state
  Initial State: Two excited state particles (e, hole, or exciton)
  They Collide!
  Energy from Particle 1 transferred to Particle 2
  Particle 1 is now in the ground state (without radiating)
  Particle 2 now has extra energy, which it tends to lose by thermalization (i.e., without radiating photons)

## Slide 32: Approach 1: Minimalist Model (Steve Payne)
Two Free Parameters:
“Strength” of Auger Quenching (Birks Parameter)
Fraction of Geminate Excitons
Only Excitons Luminesce
  Free electrons or holes get trapped / quenched
Excitation Density Assumed To Be Independent of Time
  Initial ionization density used
At High Excitation Density, Auger-Like Quenching Occurs
  Colliding excitons de-excite
  “Birks” mechanism
At Low Excitation Density, Exciton Formation Hindered
  Separated electrons & holes can’t “find each other”
  Some “geminate” excitons (formed at time zero)

## Slide 33: Excellent at Fitting Electron Response, But Can’t Predict It
SrI2(Eu)
Data from S. Payne, et al., Presentation 7805-18 at 2011 SPIE Meeting
LaBr3(Ce)
Scintillator | he/h | (dE/dx)BIRKS
Alkali Halides |  | 
CsI(Tl) | 36 % | 556 MeV/cm
CsI(Na) | 39.5 | 667
NaI(Tl) | 53.4 | 166
Simple Oxides |  | 
YAG(Ce) | 10 | 526
GYGAG(Ce) | 22 | 599
YAP(Ce) | 12 | 606
LuAG(Ce) | 8.8 | 752
LuAG(Pr) | 11 | 806
Silicate Oxides |  | 
LSO(Ce) | 13 | 185
GSO(Ce) | 7 | 556
YSO(Ce) | 13 | 167
LPS(Ce) | 5 | 125
Fluorides |  | 
CaF2(Eu) | 0 | 333
CeF3(Ce) | 0 | 313
Organics |  | 
Std Plastic | 0 | 91
Ir:Plastic | 0 | 200
Liquid | 0 | 111
Stilbene | 0 | 80
PVK | 0 | 91
Multivalent Halides |  | 
SrI2(Eu) | 24 | 454
Undoped SrI2 | 44.5 | 159
LaBr3(Ce) | 15.5 | 444
LaCl3(Ce) | 22 | 345
Tungstate |  | 
Cd(WO4) | 20 | 454

## Slide 34: Approach 2: Kinetic Model (G. Bizarri, S. Kerisit, J. Singh, A. Vasil’ev, R. Williams…)
The Processes are Described by Kinetic Rates
Many More Processes Can Participate
Different Dependences on the Ionization Density
Excitation Density Assumed To Depend on Time
  Rate equations determine propagation with time
Several Carrier Species are Present
  Free electrons, free holes, and excitons
  Some “geminate” excitons formed
Several Emission Mechanisms Occur
  Excitonic emission
  Sequential free electron & free hole capture
Several Quenching Mechanisms Occur
  Colliding excitons de-excite (“Birks” mechanism)
  Trapping on impurities / defects

## Slide 35: General Rate Equation for One Species
General Concept Seems Correct, But…
Too Many Rate Constants Needed to Describe System
Must Simplify Somehow!!!
Radiative Recombination Terms:
  First and second order (with ionization density)
Non-Radiative Recombination Terms:
  First, second, and third order (with ionization density)
Multiple Species (excitons, free electrons, free holes):
  Separate equation needed for each species
  Conversion / coupling terms also needed

## Slide 36: Model Reproduces Multiple Features
Figure from G. Bizarri, et al., Presentation at 2008 NSS/MIC, Dresden, Germany

## Slide 37: Approach 3: Diffusion Model (Richard Williams)
Electrons & Holes Diffuse After Creation
Diffusion Diameter Greatly Affects Ionization Density
Electron
Path
Hole Distribution
Electron Distribution
Non-Proportionality Depends on Volumetric Ionization Density
Bethe-Bloch Equation Gives Linear Ionization Density
Need Track Radius to Compute Volumetric Ionization Density

## Slide 38: Ratio of Electron & Hole Mobilities Important
Electron
Path
Hole Distribution
Electron Distribution
Ratio of Diameters ∝ Ratio of Mobilities
Similar Diameters  High Recombination Probability
μhole ≈ μelectron  Proportional Scintillator
μhole << μelectron
μhole ≈ μelectron

## Slide 39: Value of (Hole) Mobility Important
Sets time scale to reach equilibrium
High mobility implies that electrons & holes separate rapidly  Ionization density becomes Very low in a Very short time  Auger (non-radiative) processes are Greatly suppressed!
High Hole Mobility  Proportional Scintillator
This is Why Solid-State Detectors are Proportional!!!
Modeled Survival Probability at 10 ps
(Related to Light Yield at Low Electron E)
Measured Light Yield at Low Electron E
Figure from R. Williams, et al., SCINT11, Giessen, Germany

## Slide 40: Engineering Electron Response

## Slide 41: What Affects Electron Response? Dopant Concentration?
Dependence on Dopant Concentration is Small
LSO:Ce
LaBr3:Ce
Data from S. Payne, et al., Presentation 7805-18 at 2011 SPIE Meeting

## Slide 42: What Affects Electron Response? Crystal Structure?
Major Differences in LuAG / LSO / LPS System
Data from S. Payne, et al., Presentation 7805-18 at 2011 SPIE Meeting

## Slide 43: Sample to Sample Variation in NaI:Tl
Modeling Results: Quenching Due To Auger & Traps
Data from G. Hull, et al., IEEE Trans. Nucl. Sci. NS-56, pp. 331–336, 2009

## Slide 44: Use Model to Predict Energy Resolution if Quenching Removed in NaI:Tl
Potential to Reach 4–5% Energy Resolution @ 662 keV?
Figure from G. Bizarri, et al., Presentation I8-2 at SCINT09, Jeju Island, Korea

## Slide 45: Conclusion:
A Few Layers Peeled, but
Plenty of Onion Left!

## Slide 46: Thanks To:
John Valentine, SAIC
Gregory Bizarri, LBNL
Steve Payne, LLNL
Giulia Hull, IPN Orsay
Richard Williams, Wake Forest University
Andrey Vasil’ev, Moscow State University
And Many, Many More, Including…
IEEE NPSS Distinguished Lecturer Program
http://www.ieee-npss.org